Date of issue: Last mod. date: Product Code ETCH GLASS SERIES Description Soft glass etching translucent vinyl with metallic flakes, suitable for 5 years outdoor. Technical Data FACE MATERIAL Type Translucent vinyl Colour and Finish Etch glass effect Weight 100g/m² Thickness 80µ ADHESIVE Reference RI-ASP8 Type Permanent acrylic Min. Appl. Temp. +10°C Service Temp. -40°C/ +140°C Cohesion Excellent Tack Medium Ultimate Adhesion Very high RELEASE BACKING Type 1 side clay coated Colour and Finish White Weight 140g/m² Thickness 150µ CHEMICAL RESISTANCE Detergent Non effect ( 24 Hrs) Gasoline Non effect ( 1 Hrs ) SAE20 Motoroil Non effect ( 24 Hrs ) 10% HCI Non effect ( 10 min ) 10% NH4OH Non effect ( 10 min ) Storage The material must be stored at a temperature of 22°C +/- 2°C and 50% +/- 5% of Relative Humidity. Do not expose to direct sun light. The area must be dry and clean. Please keep the material in the original packaging when not use in order to protect it from dust and contaminations. All values presented in this data sheet are typical. The information is given in good faith but without warranty. Purchasers should carefully assess the suitability of the product for their own specific application. All specifications are subject to change without prior notice.